# Visual inspection

STN 39194-00023

# Manufacturers part Number:	……………………………………….

20220900400023

# Atlas serial number:  		……………………………………….

## Front

## Rear

Splatter type contamination

Large scrape / contamination

Small edge chip

Manufacturer has probed pads on rows A and D

20220900400023

“Splatter” on strips 505,506

which appear as a short  on the strip scan.  This suggests the problem is conductive.