# Visual inspection

# STN39229-00145

# Manufacturers part Number:	……………………………………….

20220900200145

# Atlas serial number:  		……………………………………….

## Front

## Rear

## Manufacturer has probed pads on rows A and D

1

Minor light scratching

“Minor” is used to describe a fault which is in no way a failure.

“Contamination” is matter which has wet the detector surface.

A “Scratch” is a result of mechanical damage to the detector surface.

An “edge chip” is an fault to the cut edge of the wafer .  The measurement given is the distace that the chip extends perpedicular to the wafer edge.

20220900200144

Scratch pads

Contamination and 3 deep edge chips 110um

Contamination

1

Scratch pads

20220900200145