# Visual inspection

# STN39230-00199

# Manufacturers part Number:	……………………………………….

20220900200199

# Atlas serial number:  		……………………………………….

## Front

## Rear

## Manufacturer has probed pads on rows A and D

1

Scratch pads

1

“Minor” is used to describe a fault which is in no way a failure.

“Contamination” is matter which has wet the detector surface.

A “Scratch” is a result of mechanical damage to the detector surface.

An “edge chip” or “crack”is an fault to the cut edge of the wafer .  The measurement given is the distace that the chip or crack extends

perpedicular to the wafer edge.

Edge chipping <60um

Minor light scratching worse in corners.

Scratch pads

Minor contamination x 2

2 Sets of deeper parallel scratches

20220900200199

20220900200197