# Visual inspection

# SRN39199-00082

# Manufacturers part Number:	……………………………………….

20220900300082

# Atlas serial number:  		……………………………………….

## Front

1

2 minor scratches

## Manufacturer has probed pads on rows A and D

1

Crack 190um

## Rear

Edge chipping <45um

Minor light scratching, worse in all four corners

Scratching

“Minor” is used to describe a fault which is in no way a failure.

“Contamination” is matter which has wet the detector surface.

A “Scratch” is a result of mechanical damage to the detector surface.

An “edge chip” or “crack”is an fault to the cut edge of the wafer .  The measurement given is the distace that the chip or crack extends

perpedicular to the wafer edge.

20220900300082