# Visual inspection

STN 39194-00012

# Manufacturers part Number:	……………………………………….

20220900400012

# Atlas serial number:  		……………………………………….

## Front

Bias resistors broken up

Strips 312:331, 183:189

## Rear

Green crystaline deposit

Manufacturer has probed pads on rows A and D

20220900400012